SAMPLE SPECIFICATION:

SECTION 04902-CLAY MASONRY RESTORATION

PART 1-GENERAL

1.1  SUMMARY OF WORK

A.  Extent of masonry restoration work is as shown on the Drawings and as specified herein.

1.  The drawings endeavor to show the extent of masonry restoration work required.  The

contractor shall review the Drawings, Photographs and make a Pre-bid field visit to verify all work whether shown or not shown on the Drawings.

B.  The work includes, but is not limited to:

1.  Repairing hairline cracks, microscopic cracks, cracks and voids in terra cotta construction.

2.  Patching clay masonry structures.

3.  Repairing and replacing damaged masonry.

4.  Repointing mortar joints.

5.  Reglazing of terra cotta.

C.  Related work described elsewhere:

1.  Joint sealants:  section 07900

2.  Water repellent:  section 07180

3.  Special Coatings:  section 09800

1.2  QUALITY ASSURANCE

A.  Restoration Specialist:  Work must be performed by a firm having not less than 5 years

successful experience in comparable masonry restoration projects and employing personnel

skilled in the restoration process and operations indicated.

1.  Only skilled journeymen masons who are familiar and experienced with the materials and methods specified and are familiar with the design requirements shall be used for masonry restoration.

2.  One skilled journeyman mason, trained and Certified by the specified stone repair system manufacturer, shall be present at all times during masonry restoration and shall personally direct the work.

B.  Field -Construction Mock-ups:  Prior to start of general masonry restoration, prepare the

following sample panels and sample areas on building where directed by Architect.  Obtain

Architect's acceptance of visual qualities before proceeding with the work.  Retain acceptable

panels in undisturbed condition, suitably marked, during restoration as a standard for judging

completed work.

1.  Cleaning:  Demonstrate materials and methods to be used for cleaning for each type of masonry surface and  condition on sample panels each approximately 25 sq. ft. in area.  Begin water cleaning at most gentle pressure, increase as directed by Architect.  Test adjacent non-masonry materials for possible reaction with cleaning  materials.  Allow waiting period of duration indicated, but not less than 7  calendar days after completion of sample panels for negative  reactions.

2.  Paint, Graffiti, and Metallic stain removal:  Demonstrate materials and methods to be used for paint, graffiti, and stain removal for each type of masonry surface and condition of sample panel 4 sq. ft. in area.  The  removal method or methods shall be tested on an inconspicuous area of the building.

3.  Crack Repair:  Prepare a sample area for each type of crack repair required (i.e. hairline cracks and microscopic cracks 1/64"-1/16" in size; cracks and voids larger than 1/8"). Repair shall demonstrate methods and quality of workmanship expected for crack repair.

4.  Patching:  Prepare on-building sample of each type of stone and masonry construction to be patched, rebuilt and/or replaced (e.g.  one  stone cornice unit, one window sill;  one stone base course unit and a mold of decorative stone).  Patching and mold shall  demonstrate methods and quality of workmanship expected of repair work.

5.  Masonry Repair:  Prepare sample panels of min. 9 sq. ft. in size for each  type of masonry material indicated to be patched, rebuilt or replaced.  Erect mock-up panels in-place at areas indicated to be restored/repaired, in exact locations as directed by Architect, to demonstrate quality of materials and workmanship.

6.  Repointing:  Prepare 2 separate sample areas of approximately 5' high by 5' wide for each type of repointing required, one for demonstrating methods and quality of workmanship expected in removal of mortar from joints and the other for demonstrating quality of materials and workmanship expected in pointing mortar joints.  Sample areas shall be located in an inconspicuous yet readily accessible place.

C.  Patching, Repointing and coating work:  The samples of each type of repair work shall be

done in an area that will be exposed to the same weathering conditions as the building.  Allow

samples to cure at least three days before obtaining acceptance of color,  texture and detailing

match. Samples shall be viewed from an approved distance.

D.   Source of Materials:  Obtain materials for Patching, coating, sealing, crack repair and

repointing from a single manufacturer source to ensure match quality, color, texture and

detailing.

1.3  SUBMITTALS

A.  Product Data:  Submit manufacturer's technical data for each product specified including

recommendations for their application and use.  Include test data and certifications

substantiating that products comply with requirements.

B.  Submit the following items in time to prevent delay of the work and to allow adequate time

for review and resubmittals, if needed. Do not order materials or start work before receiving the

written approval:

1.  Written certificates from the patching materials manufacturer should be submitted stating that all installers of the patching material have successfully completed a training workshop for installation of the patching material, or have met alternative workmanship qualifications acceptable to the manufacturer, or provide written certification from the manufacturer that on-site training services have been contracted for.

2.  Samples of all specified materials and Material Safety Data Sheets (MSDS) as appropriate.

3.  Certificates, except where the material is labeled with such certification, by the producers, of the materials, that all materials supplied comply with all the requirements of these specifications and the appropriate standards.

4.  Color-match patch samples fabricated on pieces of appropriate masonry from or on the

building using the specified repair mortar as required.

5.  Written verification that all specified items will be used.  Provided purchase orders, shipping tickets, receipts, etc. to prove that the specified materials were ordered and received.

C.  Restoration Program:  Submit written program for each phase of restoration process

including protection of surrounding material on building and site during operations.  Describe

in detail material, methods and equipment to be used for each phase of restoration work.

D.  SUBSTITUTIONS

1. If alternative methods and materials to those indicated are proposed for any phase of 	restoration work, provide written description, including evidence of at least 10 years' successful use on other, comparable projects, and program of testing to demonstrate effectiveness for use on this project. Provide documentation showing compliance with the requirements for substitutions and the following information:

a. Coordination information, including a list of changes needed to other work that will be necessary to accomodate the substitution.

b. A comparison of the substitution with the specified products and methods, including performance, weight, size, durability, and visual effect.

c. Product data, including specifications for products and installation procedures.

d. Samples, where applicable, or as requested.

e. A statement indicating the effect on the Contractor's Construction Schedule compared to the schedule without approval of the substitution. Indicate the effect of the substitution on Contract completion time.

f. Cost information, including a proposal of the net change, if any, in the contract sum.

g. Certification that the substitution conforms to the contract documents and is appropriate for the applications indicated. Material substitution requests must be accompanied by independent laboratory test reports from a lab designated by the architect to establish equivalent performance levels and specification compliance. Testing shall be paid for by the submitting party.

h. The Contractor's waiver of rights to additional payment or time that may become necessary because of the failure of the substitution to perform adequately.

1.4  DELIVERY, STORAGE AND HANDLING:

A.  Deliver  materials to site in manufacturer's original unopened containers and packaging,

bearing labels as to type and names of products and manufacturers.

B.  Deliver and store restoration material in manufacturer's original, unopened containers with

the grade, batch and production data shown on the container or packaging.

C.  Protect restoration materials during storage and construction from wetting by rain, snow or

ground water, and from staining or intermixture with earth or other types of materials.

D.  Protect grout, mortar and other materials from deterioration by moisture and temperature.

Store in a dry location or in waterproof containers.  Keep containers tightly closed and away

from open flames.  Protect liquid components from freezing.  Comply with manufacturer's

recommendations for minimum and maximum temperature requirements for storage.

F.  Comply with the manufacturer's written specifications and recommendations  for  mixing,

application, and curing of grouts and patching materials.

1.5  PROTECTION / SITE CONDITIONS

A.  Protect persons, motor vehicles, building site and surrounding buildings from injury

resulting from masonry restoration work.

B.  Clean masonry surfaces only when air temperatures are above 40 degrees F (4 deg. C) and

will remain so until masonry has dried out, but for not less than 7 days after completion of

cleaning.

C.  Do not perform any masonry patching unless air temperatures are between 50 degrees

Fahrenheit (10 deg. C) and 90 degrees Fahrenheit (32deg. C) and will remain so for at least 48

hours after completion of work.

D.  Prevent masonry patching materials from staining the face of masonry or other surfaces to

be left exposed.  Immediately remove all patching materials that come in contact with such

surfaces.

E.  Cover partially completed work when work is not in progress.

F.  Protect sills, ledges and projections from droppings.

1.6  SEQUENCING / SCHEDULING:

A.  Perform masonry restoration work in the following sequence:

1.  Repair and/or replace existing roofing, flashing, drains and leaders as indicated.

2.  Remove paint, stains and plant material from all masonry surfaces.

3.  Rake-out existing mortar from joints of masonry indicated to be restored.

4.  Repoint existing mortar joints of masonry indicated to be repointed.

5.  Pressure wash building exterior.

6.  Patch and repair existing stone structures as indicated, including replacing damaged

masonry units with new masonry units where indicated.

7.  Provide water repellent treatment for masonry structures as indicated. Water

repellent/consolidant is specified in Section 07180.

8.  Provide special coating over indicated sections to match the existing color of the original, adjacent masonry  units.  Special coating is specified in Section 09800.

PART 2 - PRODUCTS

2.1 REPOINTING MORTAR MATERIALS:

A. Repointing mortar shall be a pre-mixed, pre-colored cement-lime based mixture formulated

to comply with the requirements of ASTM C-270 Type N mortar.

1. Products: The following shall be assumed to meet the quality and performance requirements specified:

a. "SPEC-JOINT 46", by Edison Coatings, Inc., Plainville, CT, (800)697-8055, or approved equal.

b.  If proposed equal is submitted, thorough lab testing shall be required to establish equivalent performance levels.   An independent testing laboratory shall be utilized as determined by the Architect and paid for by the submitting party.

2.2 CRACK INJECTION MATERIALS

A. Cementitious crack filler shall be an ultra-fine, superplasticized, polymer- modified injection

grout. Cementitious grout shall be suitable for application in wet or dry cracks, shall develop

direct tensile bond strength of 100 psi minimum, shall exhibit less than 0.06% drying shrinkage,

and shall have a linear coefficient of thermal expansion of 0.000004 to 0.000008 inches/inch

per degree Fahrenheit.

1. Products: The following shall be assumed to meet the quality and performance requirements specified:

a. PUMP-X 53i, as manufactured by Edison Coatings, Inc., Plainville, CT, Phone (800) 697-8055.

B. Flexible epoxy crack filler shall be an ultra-low viscosity, two component, 100% solids

elastomeric epoxy, suitable for injection into dry or damp cracks. Product shall have a minimum

of 100% elongation, 1200 psi tensile strength and 300 psi direct tensile bond strength. Mix

viscosity shall not exceed 200 cps at 75 degrees Fahrenheit.

1. Products: The following shall be assumed to meet the quality and performance requirements specified:

a. FLEXI-SEAL 510, as manufactured by Edison Coatings, Inc., Plainville, CT. Phone (800) 697-8055.

2.3  PATCHING MATERIAL:

A.  Patching material shall be a premixed, cementitious material with acrylic latex-modifier,

formulated to match the color and texture of the existing cast stone. Material must be vapor

permeable, frost and salt resistant, shall develop direct tensile bond strength of 150 psi

minimum, shall exhibit less than 0.06% drying shrinkage, and shall have a linear coefficient of

thermal expansion of 0.000004 to 0.000007 inches/inch per degree Fahrenheit. Material shall be

compatible with substrate, including but not limited to, porosity, tensile, and compressive

strength. Modulus of elasticity shall be 50,000 to 100,000 psi. Non-latex mortars shall be

unacceptable. Material shall have a minimum 10-year successful performance history for similar

projects.

1.  Products:  Subject to compliance with requirements, provide the following:

a.  "Custom System 45" by Edison Coatings, Inc. , Waterbury, Ct (800) 697-8055.

b.  If proposed substitute is submitted, thorough lab testing shall be required to establish equivalent performance levels. An independent testing laboratory shall be utilized as determined by the Architect and paid for by the submitting party.

2.4  RUST INHIBITIVE COATING/PRIMER

A.  Rust inhibitor/primer for steel reinforcement shall be a pre-packaged, 2-component, acrylic

latex-modified silica fume-cement mortar.

1. Products: Subject to compliance with requirements, provide the following:

a. "SYSTEM 49 CPBA", by Edison Coatings, Inc., Plainville, CT. (800)697-8055, or an approved equal.

b.  If proposed equal is submitted, thorough lab testing shall be required to establish equivalent performance levels. An independent testing laboratory shall be utilized as determined by the Architect and paid for by the submitting party.

2.6  REINFORCING MATERIALS

A.  Pins / Threaded rods:  Type and size are specified herein and as indicated on the

Contract Drawings, if not indicated, as per patching materials manufacturer's recommendation.

Anchors and dowels shall be fabricated from ANSI Type 302/304 stainless steel.

B.  Mechanical anchors and dowels (for deep repairs and overhanging repairs):

Stainless steel threaded road (ASTM F-593) with a diameter as indicated on  Contract Drawings,

bent and cut to lengths required to achieve embedments shown on Contract Drawings.  Cut end

of rod square.

C.  Adhesive:  Adhesive shall be a two component, flexibilized epoxy gel, with minimum 4%

elongation, 300 psi direct tensile bond strength, 10,000 psi tensile strength. Product shall be

applicable to metals, masonry, concrete and other substrates as required, and shall be

appropriate for use at ambient temperatures from zero degrees to 100 degrees Fahrenheit (-18

to 38 degrees Centigrade).

1. Products: Subject to compliance with requirements, provide the following:

a. FLEXI-WELD 520T, as manufactured by Edison Coatings, Inc., Plainville, CT (800) 697-8055.

b.  If proposed equal is submitted, thorough lab testing shall be required to establish equivalent performance levels. An independent testing laboratory shall be utilized as determined by the Architect and paid for by the submitting party.

D. Breathable Elastomeric Coating: Breathable elastomeric coating shall be a one-component,

internally plasticized acrylic elastomer, with min. 300% elongation at 75 degrees Fahrenheit and

100% elongation at 0 degrees Fahrenheit. Minimum solids content shall be 72% . Glass transition

temperature shall be a maximum of 15 degrees below zero Fahrenheit.

1. Products: Subject to compliance with requirements, provide the following:

a. ELASTOWALL 351, as manufactured by Edison Coatings, Inc., Plainville, CT (800) 697-8055.

E. Terra Cotta Glaze Replacement: Glaze replacement shall be a breathable, one component, self-

crosslinking aliphatic polyurethane emulsion with minimum 50% elongation, 5000 psi tensile

strength, 48 Sward hardness and minimum 1500 hours UV stability (Fadeometer).

1. Products: Subject to compliance with requirements, provide the following:

a. AQUATHANE UA-210NCL with Type G Additive, as manufactured by Edison Coatings, Inc., Plainville, CT (800) 697- 8055.

F. Water Repellent/Consolidant: Water repellent/light consolidant shall be a breathable, two

component, proprietary self-crosslinking hybrid system. Product shall be colorless, low

viscosity, two component penetrating treatment with minimum 96% moisture vapor

transmission per Oklahoma DOT method, maximum 1% water absorption per Ontario MTC

method, and which meets the freeze-thaw requirements of Ontario MTC (50 cycles) and the

wind-driven rain resistance requirements of US Federal Specification TT-C-555B. Product shall

be non-yellowing and UV resistant for a minimum 1500 hours per ASTM G53-84. Product shall be formulated using VOC-exempt, non-HAPS solvent to meet local, state and federal regulations.

1. Products: Subject to compliance with requirements, provide the following:

a. SYSTEM 90-II, as manufactured by Edison Coatings, Inc., Plainville, CT (800) 697-8055.

PART 3 - EXECUTION

3.1  WORKMANSHIP OF PATCHING MATERIAL:

A.  Patching material workmanship shall comply with all applicable recommendations of

material manufacturer's written specifications and requirements and/or as modified in this and

following sections.

B.  Mixing of patching material:  Mix the patching material in accordance with Manufacturer's

printed instructions.

C.  Do not use any additives, such as bonding agents, accelerators, or retarders, in the patching

material without prior written approval from the Manufacturer.

3.2  SURFACE PREPARATION:  (for all patching work)

A.  Patching and repair work for spalled and deteriorated materials (i.e. stone and masonry

constructions) shall be accomplished with the approved Patching material, according to

manufacturer's printed instructions and as specified herein.

B.  At areas to receive patches, remove all loose, spalled and deteriorating materials.  If required

cut away an additional 1/4 to 1/2 inch of the substrate that may be in the process of

deteriorating and to ensure the surface to be patched is solid and stable.  "Sound" substrate

with a hammer to verify its integrity.

C.  Remove any soil, mortar, and other debris or foreign material from areas to receive Patch.

D.  Once the deteriorated material in a spalled area has been removed, rust on the exposed

reinforcements must be removed by wire brush or local sandblasting.  Remove material around

reinforcement to provide a minimum  of 1/2 inch clearance.  Apply an epoxy coating or an

approved rust-preventive agent to cleaned reinforcement.

E.  Remove reinforcements that are severely corroded, loose or are of no structural value.

Removal shall be done upon evaluation of the field condition and approval by the Architect.

Proved new supplemental reinforcing bars where required.  Repair damage to substrate

resulting from removal by Patching with the approved patching material.

F.  Cut out sections shall be squared off at the edges.  Do not overcut corners of the patch; stop

short of corner and chip out remainder by hand without  damaging surrounding masonry.  Do

not allow any feathered edges in the patch areas.

G.  Roughen the substrate surface as necessary to achieve the surface roughness required by

manufacturer for good bond, but do not damage the substrate surface.  Moisten substrate

surfaces as per manufacturer's directions.

H.  For very dry or porous surfaces, pre-wet the substrate ahead of time to prevent the

substrate from drawing moisture out of the patch too quickly. Re-wet the surface just before

applying the patching material.

I. Prepare and mix a slurry coat consisting of 2 parts patching material dry component and one part liquid component. Apply to prepared and pre-dampened cavity by brush, working slurry into corners, edges and surface depressions. Apply as a thin coating only, avoiding heavy build-up or filling of surface depressions.

3.3  PATCHING REPAIR WORK:

A.  Prepare and mix Patching material in accordance with manufacturer's directions.

B.  Patching material shall be applied by trowel, casting-in-place or other techniques

recommended by approved materials manufacturer for each specific field conditon.

C.  Air, surface and product temperature must all be above minimum temperature of 50 deg F

(10 deg C) at time of application and must be maintained above minimum until product has

dried thoroughly.

D.  Apply Patching material in one layer or several layers according to the depth of the repairs.

Comply with manufacturer's instructions when applying multiple layers for thickness of each

layer, setting-up time for each layer, surface preparation between layers, etc., to ensure sound

adhesion between layers.  Final application of repair mortar shall be at the desired surface level and shall be tooled, shaped or carved as required to achieve proper surface profile and texture. Surfaces shall be tooled to replicate the texture, and detailing of the original surface. Do not sponge float the patch. Keep tools clean by frequent washing in clean water, but remove excess water to avoid introducing water into patch surfaces.

E.  Under hot conditions, as directed by Manufacturer, cover and cure repaired areas in

accordance with manufacturer's  directions.  Keep patches moist and out of direct sun for at least the first day.

F.  To avoid rapid evaporation, do not patch in direct sunlight.  If necessary, cover work with

tarpaulin or wet burlap.

3.4  PATCHING FOR DEEP OR OVERHANGING REPAIR:

A.  At areas of large, deep and overhanging repairs the installation of mechanical keying or

anchoring is required.  The decision whether to anchor and how frequently to provide anchors

shall be based on structural requirements, the conditions of the substrate, patch dimensions

and weight, and the extent to which patch integrity will rely on adhesion alone.  Typical

procedures are outlined in this section and shall be modified as recommended.

B.  Drill 1/4" to 1/2" diameter holes at various angles, spaced 4 to 6 inches apart in staggered

rows. Clean holes using compressed, oil-free air.

C.  Insert threaded nylon or stainless steel rods into drilled holes.  Span rods between holes, and extending far from substrate surface to be completely surrounded with patching material.  At least 3/4" of patching material is placed over the rods, which are secured into the holes with the specified adhesive.

D.  Prepare and mix patching material in accordance with manufacturer's directions.  Comply

with all safety precautions, environmental limitations and work time limitations.

E.  Dampen patch area  immediately prior to application of patching material to create a good

bond. Using a masonry brush, apply bondcoat to patch area, working into corners, edges and

profile. Apply bond coat only to area of patch that can be covered with patch material mix

before bond coat dries.  Work bond coat into pieces of the substrate and under and around

mechanical anchors.  Do not apply excess bond coat; do not leave standing in puddles on the

substrate. Do not allow bond coat material to run down onto surfaces which will not be

repaired.

F.  Apply patching material to deep sections by building up in a series of multiple lifts. Comply

with manufacturer's instructions for thickness of each layer, setting-up time for each layer, and

surface preparation between layers to ensure sound restoration.  Work patching material into all

corners of patch  area and under and around mechanical anchors; including the existing coated

reinforcements.

G.  To re-create original ornamentation, apply an extra-thick patch.  Then after the patch is

partially cured the patching material shall be carved, using molding profiles and/or straight

edges to restore original ornamentation.  In all cases, finish patch so that it is as indistinguishable as possible from adjacent surfaces.

H.  Clean any patching material residue from area surrounding the patch by sponging as many

times as necessary with clean water.  This should be done before patching material sets.

I.  Moisten, cover and cure repaired areas in accordance with manufacturer's directions.

3.8   REPAIRING CRACKS AND VOIDS

A.  Prepare cracked area in accordance to manufacturer's written instructions. Typical

procedures are outlined in this section and shall be modified according to approved materials

manufacturer.

B.  Crack repair for hairline and microscopic cracks:

1.  Inject flexible epoxy crack repair material into designated cracks, using syringes, grouting pumps, or other types of injection apparatus suitable for size of crack, distance crack injection material must travel and viscosity of material used.  Seal surfaces as required to prevent crack injection material from leaking out and to facilitate pumping.  Take caution not to strain the face of adjacent surfaces.

2.  Immediately wipe spills off surfaces with clean rag and compatible solvent and allow injection material to cure as required.

C.  Crack repair for cracks larger that 1/16" and voids larger that 1/8" mm:

1.  Remove loose and spalling materials, cut into crack to a minimum depth of 3/8 inches and a width of 3/16 inch.  If embedded reinforcements are rusted then cut-material deep enough to expose the rusting reinforcements and remove material around reinforcement to provide a minimum of 3/4 inch clearance for patch material.

2.  Clean and coat exposed reinforcements at patch work with an approved rust- preventative agent.

3.  Fill enlarged areas of crack repair with patching material, following repair procedures outlined in this section under Part 3.  "Patch for typical repair work" and/or Part 3. "Patching for deep or overhanging repair."

D. Inject cementitious crack repair material into designated voids and cracks, using syringes,

grouting pumps, or other types of injection apparatus suitable for size of crack, distance crack

repair material must travel and viscosity of material used.  Seal surfaces as required to prevent

crack injection material from leaking out and to facilitate pumping.  Take caution not to strain

the face of adjacent surfaces. Immediately wipe spills off surfaces with clean rag and compatible

solvent.

E. Unacceptable patches are defined as those with hairline cracks or showing separation from

repair edges, or on which "hollow spots" can be detected by light impact.  Remove unsound patches and refill to provide patches free of those defects.

F. Final Cleaning: No steam cleaning or additional pressure cleaning shall be performed within

28 days of patch installation. No acid or alkali cleaning agents shall be used. If haziness

develops due to curing conditions, soak patch surfaces with methylene chloride or other

VOC-compliant solvent or other curing aid as recommended and/or approved by patch

manufacturer.